Product Information Data Sheet

- PRODUCT DESCRIPTION:

Epo-Crete Slurry is a four-component, urethane flooring system. It is a screed rake applied slurry system, with broadcast aggregate, installed at ¼ inch (250 mils). Epo-Crete Slurry is U.S.D.A. acceptable for food processing plants and has excellent resistance to thermal shock, many acids, caustics, detergents and other corrosive materials. Epo-Crete Slurry can be applied at temperature ranges from 40°F to 90°F. (4.4°C – 32.2 °C)

ADVANTAGES:

- Thermal Shock Resistant

- Prepackaged, Applicator Friendly

- Excellent Adhesion

- Short Down Time – Quick Cure

- Easy to clean, U.S.D.A. acceptable.

- Chemical Resistant

- Environmentally safe.

- Moderate Slip Resistance – 30 mesh aggregate

USES:

- Food Production Plants

- Oven and Fryer Lines

- Coolers and Freezers

- Forklift Aisle-ways

- Chemical Spill Containment Areas

- Industrial Production Facilities

- Agricultural Facilities

PACKAGING AND COVERAGE:

Epo-Crete Slurry – packaged in batches,

- supplied by the UNIT - consisting of the following -

2 batch unit – covers approximately 60 sq. ft. (5.57 m²) at

¼ inch (6.35 mm), consisting of the following -

- 2 containers - Part A (resin)

- 2 containers - Part B (hardener)

- 2 bags - Part C (chemical resistant aggregate)

- 50# - Part D (broadcast aggregate)

20 batch unit – covers approximately 600 sq. ft. (55.74 m²) at

¼ inch (6.35 mm), consisting of the following -

- 20 containers - Part A (resin)

- 20 containers - Part B (hardener)

- 20 bags - Part C (chemical resistant aggregate)

- 500# - Part D (broadcast aggregate)

SURFACE PREPARATION:

Epo-Crete Slurry may be installed only on clean, sound substrates

Concrete: New concrete must be cured a minimum of 28 days. All coatings, oils, grease and unsound concrete must be removed. Concrete surfaces must then be mechanically abraded with a scarifier, shot blaster, or like equipment, to remove surface laitance. A good bonding tooth, the texture of 60 grit sandpaper, is desired for proper adhesion to the substrate.

| MIXING: TECHNICAL DATA |  |
| --- | --- |
| Solids by Content: | Weight:100% Volume:100% |
| Colors: | Gray, Red, Black |
| Compressive Strength (ASTM C-579)<resin>: | 8,100 psi |
| Tensile Strength (ASTM D-638) <resin>: | 950 psi |
| Bond Strength (ASTM C-321): | Greater than 350 psi; 100%concrete failure |
| Working Time at 75°F (24°C) (ASTM C-308): | 20-30 minutes |
| Flexural Strength (ASTM C- 580) <resin>: | 1,900 psi |
| Coefficient of Thermal Expansion: | 1.1 x 10-5 in./in./oF |
| Impact Strength: | 120 in./lbs. |
| Modulus of Elasticity (ASTM C-580): | 1.7 x 105 psi |
| Indentation(MIL-D-3134F): | No Indentation |
| Flammability: | Does not support combustion |
| Shelf Life: | 6 months (store at Minimum temperatures of 50°F) Part A and B may crystallize below 50°F |

Prior to mixing, materials should be stored at 70°F (21°C) at

least 48 hours.

Mortar: Empty the entire contents of Part A and Part B into a pail and mix thoroughly for two minutes. Slowly add the entire contents of Part C (aggregate) and continue mixing the three components (Part A, B, and C) for an additional two minutes. If mortar is allowed to sit in the mixer, the working time of the system will be reduced.

- APPLICATION:

DO NOT APPLY IF RELATIVE HUMIDITY IS ABOVE 85%. Substrate temperature should be 65°-80°F (18°-26°C) during installation and for 28 days thereafter for complete cure. Immediately after mixing, pour the entire batch onto the floor and spread evenly with a screed rake and back roll with a looped roller to smooth any irregularities. Leaving a wet edge for the next batch, broadcast the Part D aggregate into the freshly leveled surface. Repeat process until entire floor is covered. After Epo-Crete Slurry has hardened overnight (approximately 12-18 hours), sweep off excess Part D from the broadcast coat. Unless otherwise specified, the Epo-Crete Slurry flooring system is designed to follow the existing contour of the floor.

CURE TIME:

Epo-Crete Slurry will harden to foot traffic in 8-12 hours at 75°F (24°C). Maximum chemical resistance and physical properties will be attained after 28 days at 75°F (24°C).

CLEANING:

Cured or hardened Epo-Crete Slurry will bond to practically all surfaces and is extremely difficult to remove. Clean all tools and mixer immediately after use with Solvent 101.

SAFETY:

Avoid skin contact. If eye contact occurs, flush with water and consult a physician immediately. Keep work areas well ventilated. Never seal a container of mixed Part A and B, as the continuing exothermic reaction may cause container to explode. Epo-Crete Slurry Safety Data Sheets are available upon request.

Warning:

Epo-Crete Slurry may crystallize when exposed to temperatures

below 50° F (10° C) for extended periods of time. Epo-Crete Slurry should not be exposed to freezing temperatures. The prepackaged components are NOT freeze / thaw stable.

ADDITIONAL INFORMATION:

For additional information or application help regarding this product or others please contact Vanberg Specialized Coatings at 1-800-874-0631 or www.vanbergcoatings.com